D607162002

Today we have started to work from south to north side to see surroundings of the furnace. First, we opened new section on the south side of the furnace. On this part of the new section that includes Loc 9 and loc 23, was the same as the Loc 17 (zemin). We thought, the furnace was built on the Loc 17. Having kept brick, we took down loc 19 same as the Loc17. And we tried to take down loc 29same as the Loc 17 also. But we could not continue to take down because we found pieces of the furnace. Then we turned on loc6 and we took 3cm down. Besides, we excavated new area that was plastered with clay (the color was yellowish brown) on the west side of the Loc 16. It was probably part of the furnace. After that we took down 2 cm on Loc 11.(we did not see anything).Today also we got first carbon sample on Loc 29(# 20) besides, we found many slag samples  loc 9 (# 23), Loc 29 (#25-#17). Moreover, we took soil samples from each locus.

At the end of the day, we took spider shot (surrounding of the furnace).